**Beacon Signal Vac AXT Pump Oils**

|  |
| --- |
| Product Application: |

Beacon Signal Vac AXT Pump Oils are industrial grade compressor/vacuum lubricants specially formulated from high VI paraffinic and with a blend of polyalphaolefin base stocks.

Beacon Lubricants Signal Vac AXT Pump Oils are characterized by outstanding rust protection, low deposit formation, excellent demulsibility, and low air entrainment, excellent anti-foam properties. Recommended drain intervals in excess of 8,000 hours or more under normal operating conditions.

|  |
| --- |
| Package Size: |

Bulk, Drums, Pails

|  |
| --- |
| Meets or Exceeds the following Specifications: |

Cincinnati Milacron Heat Test A

Abex-Denison HF-1

Cincinnati Milacron P-38, P-54, P-57

Mil-H-17672D

General Electric GEK-32568

AGMA Specification for R&O Gear Oils

ASTM D-943 (5000 hours)

|  |
| --- |
| Typical Characteristics: |

**ISO GRADE 32 46 68 100 150**

Gravity, Degrees API 30 30 32 30 29.5

AGMA Number -- 1 2 3 4

Viscosity Index (Min.) 140 145 155 170 180

Viscosity

cSt @ 100 °C 5.4 6.5 8.4 11 14

cSt @ 40 °C 32.2 46 65 98 145

Flash Point, COC, °F 502 507 509 511 515

Pour Point, °F -55 -45 -40 -40 -35