**Signal Volt 60**

|  |
| --- |
| Product Application: |

Signal Volt 60 is a superior quality, technical grade, fully inhibited transformer oil designed to meet the operating requirements of transformers and other oil filled electrical equipment. It meets the requirements of ASTM D 3487 Type II fluid, providing good performance in transformers, circuit breakers, switches, and capacitors.

Signal volt 60 is manufactured from carefully selected base stocks favored by the domestic and international power industries under stringently controlled manufacturing conditions. It meets the demanding requirements of the ANSI/ASTM D 3487 specification for electrical insulating oils.

|  |
| --- |
| Package Size: |

Drums, Pails

|  |
| --- |
| Features and Advantages: |

\*Excellent oxidation stability helps to extend lubricant service life and reduce maintenance costs

\*Great low temperature performance helps enable easy low temperature start up

\*Industry proven insulating properties   
\*Meets the requirements of ASTM D 3487 Type ii (2000)

|  |
| --- |
| Typical Characteristics: |

Color (ASTM D 1500) L0.5

Viscosity, cSt. @ 40°C 3.9-4.5

Viscosity, cSt. @ 100°C 2.3

Flash Point, °C, ASTM D 92 285

Pour Point , °C, ASTM D97 < 40°C

Visit us at – www.beaconlubricants.com