**Stoddard Solvent**

|  |
| --- |
| Product Application: |

Stoddard Solvent is used for a parts cleaner, paint thinner, charcoal starter, used in hand cleaners, asphalt cutbacks, and industrial cleaners

|  |
| --- |
| Package Size: |

2.5 gallons, 5 gallon pail, 55 gallon drum

|  |
| --- |
| Typical Characteristics:  |

ASTM Method Description Specification

 Minimum Maximum Typical

 LB/GAL 6.40 6.47 6.43

D4052 Gravity, API 50.4 52.3 51.4

D56 Flash Point, °F(°C) 105(41)

D611 Aniline Point, °C 65

D1133 Kauri Butanol Value 32.52

D5949 Pour point, °C(°F) -60 (-76)

D2622 Sulfur, WT % 0.0050 <0.0005

D156 Color, Saybolt +30

D86 Distillation, °F

 IBP 310

 5% 310 322

 50% 341

 95% 375

 EBP 410 393

D1319 Flour. Indicator Analysis

 Aromatics, Vol % 10.5

 Olefins, Vol % 0.4

 Saturates, Vol % 89.1