**Beacon Anti-Rust 156**

|  |
| --- |
| Product Application: |

Beacon Anti-Rust 156 is premium quality transparent lightly colored water displacing non-staining rust and corrosion preventative. It is formulated using the latest approved technology in light-bodied oils and hydro treated solvents blended with polar corrosion inhibitors, water displacing and fingerprint neutralizing agents.

Anti-Rust 156 is well suited for the thin film protection of parts between machining where water-based coolants has been used. It has a light viscosity which assures adequate coverage of metal surfaces while allowing excess fluid to drain rapidly thus allowing for a smooth efficient application.

Beacon Anti-Rust 156 is an excellent light bodied nonconductive rust and corrosion preventative for finished parts in dry storage or for adequately covered or bagged transport.

|  |
| --- |
| Meets or Exceeds that following Specifications: |

Military Specifications PRF16173E

Military Specifications MIL-C-15074E

|  |
| --- |
| Theoretical Coverage: |

2,500 sq. ft. /gallon

|  |
| --- |
| Typical Characteristics: |

Specific Gravity @ 60 °F .82

Flash Point, COC, °F 160

Pour Point, °F -20

Appearance Light Amber

Film Thickness .15 mil

Cure Time- Approximately 2 hours

|  |
| --- |
| Corrosion Test Results: |

ASTM B-117 5 % salt spray (hours) 116

ASTM D-1748 100 % relative humidity (hours) 1825

Corrosion Test Mil-C-23411 pass

Corrosion Test Mil-C-81309 pass

Water displacement pass

Stain test (Mil-C-22235A) pass

Visit us at – www.beaconlubricants.com