**Signal Cut 211B**

|  |
| --- |
| Product Application: |

Signal Cut 211B is a specially formulated oil free fully synthetic metalworking fluid designed to excel in light high-speed machining and all types of grinding application encountered in modern machining.

Signal Cut 211B is designed to machine all types of materials from plasticized polymer to ferrous and non-ferrous metals.

Signal Cut 211B is an environmentally responsible product that contains no chlorine, nitrites, heavy metal, phenols or diethanolamines.

|  |
| --- |
| Package Size: |

Drums, Pails

|  |
| --- |
| Recommended Concentrations: |

Surface Grinding 2-3% (30:1 to 20:1)

Cylindrical Grinding 3-5% (30:1 to 20:1)

Centerless Grinding 3-5% (30:1 to 20:1)

Milling, Tuning 4-5% (25:1 to 20:1)

|  |
| --- |
| Features and Advantages: |

\*Excellent microbial control – extended sump life

\*Complete oil rejecting capabilities (tramp oils)

\*Provides excellent corrosion control

\*Provides unequaled extreme pressure properties

\*Operator friendly, easy to mix, mild to skin

\*Very low foam potential even in dead soft water

\*Excellent separation from swarth material

|  |
| --- |
| Typical Characteristics: |

Color Blue

Specific Gravity

(20°C) 1.1

pH @ 20:1 Dilution 9.5

Refractometer Reading 1.0

@ 20:1 Dilution (Brix)

Corrosion Test (IP287) Break Point % 3.3

Visit us at – www.beaconlubricants.com