**Beacon Signal Cut 375**

|  |
| --- |
| Product Application: |

Beacon Signal Cut 375 is a lightly colored low odor non-corrosive, non-staining mineral oil based cutting fluid formulated for medium to heavy duty machining applications.

Signal Cut 375 is formulated utilizing the latest high quality base stocks and select synthetic esters to provide the necessary medium for excellent non-corrosive machining performance in any and all high speed machining applications. It’s versatility as a cutting fluid, and machining tool lubricants makes it an excellent choice for screw cutting lathes and other cutting machinery for which the manufacturer recommends a single multi-functional product.

Signal Cut 375 is a multi-purpose product that contains no active sulfur. Its versatility as a cutting fluid and machining tool lubricant makes it an excellent choice for screw cutting lathes and other cutting machinery for which the manufacturer recommends a single multi-functional product.

|  |
| --- |
| Package Size: |

Bulk, Drums, Pails

|  |
| --- |
| Features and Advantages: |

\*Superior frictional properties

\*Carbide tooling compatible

\*Mist suppressant minimizes fogging/stray mist

\*Non-staining technology/non-corrosive

|  |
| --- |
| Typical Characteristics:  |

Color Amber

Specific Gravity .877

Viscosity SUS @100 °F 180

Flash Point, C.O.C., °F 400

Pour Point, °F 10

Synthetic Ester 9.85

Visit us at – www.beaconlubricants.com