**Beacon Signal Film 68**

|  |
| --- |
| Product Application: |

Beacon Signal Film 68 is a full-bodied neutral mineral oil based rust preventative and penetrant lubricant developed for use as a corrosion protectant in automotive and commercial settings. Such as “oil undercoating.”

This product utilizes the latest cutting edge technology in water impervious base stocks, rust and corrosion inhibitors and plasticized polymer tackifiers that allows for uniform film thickness and ease of application while leaving a tenacious protective film to any surface applied.

This durable product prevents and in many cases slows and halts oxidizing rust in the harshest of winter climates.

|  |
| --- |
| Recommended methods of application: |

\*Air operated undercoating equipment  
\*Air less spray equipment

\*Brush

|  |
| --- |
| Theoretical Coverage: |

\*Average use is 1.0 – 1.5 gallons per average size vehicle.

|  |
| --- |
| Typical Characteristics: |

SAE Grade 20w

Specific Gravity @ 60 °F .88

Flash Point 388 °F

Pour Point 10 °F

Appearance Amber

Cure Time 1.0 Hour

|  |
| --- |
| Clean up recommendations: |

\*Easily cleaned up with warm soapy water or mineral spirits

|  |
| --- |
| Package Sizes Available: |

2.5 gallon containers, 5 gallon pails, 55 gallon drums

Visit us at – www.beaconlubricants.com