**Beacon Signal Plex EP2 Green**

|  |
| --- |
| Product Application:  |

Beacon Signal Plex EP2 Green is a commercial grade heavy-duty highly tacky lithium complex grease for use in settings where a premium, tackified, extended life grease is required.

This product excels in areas such as industrial, marine, farm, and excavating applications where critical tacky lubrication is required.

With its heavy fortified base stocks and highly tacky nature, this product is best suited for highly loaded applications at slow-to-moderate speeds.

|  |
| --- |
| Package Size:  |

Drums, Kegs, Cases

|  |
| --- |
| Performance Features: |

\*Highly Tacky

\*Excellent water resistance

\*Superb high temperature resistance

\*Excellent extreme pressure properties

|  |
| --- |
| Typical Characteristics:  |

Soap Type Lithium Complex

Color Green

Structure Tacky

Penetration at 77 °F

 60 strokes 280

 10,000 strokes 290

 100,000 strokes 300

Dropping Point, °F 500

Timken OK Load, lbs, min 80

Oxidation Stability

 100 hrs. @ 210 °F, psi loss 8.0

Rust Prevention Rating 1,1,1

Water Washout,

 @ 175 °F, % 1.1