**Beacon Signalplex EP White**

|  |
| --- |
| Product Application: |

Beacon Signalplex EP White is a high quality, industrial grade, multi-purpose lithium complex grease. This grease meets the lubrication requirements of plain and anti-friction bearings, gears, and couplings in general industrial applications. It is tough, versatile and long lasting. Beacon Signalplex EP White features multi-purpose use, good water resistance, high temperature performance, excellent oxidation resistance, good rust protection and fortified extreme pressure properties.

|  |
| --- |
| Package Size:  |

Drums, Kegs, Pails, Cases

|  |
| --- |
| Performance Features: |

\*Excellent shear & oxidative stability

\*Multi-purpose use

\*Excellent water resistance

\*Superb high temperature resistance

|  |
| --- |
| Typical Characteristics:  |

**NLGI GRADE 1 2**

Penetration at 77 ˚ F

60 strokes 310 280

10,000 strokes 320 285

100,000 strokes 340 290

Dropping Point, ˚ F 400 425

Timken OK Load, lbs, min 50 50

Four Ball EP

 Weld Point kg 250 250

Soap Type Lithium Complex

Color White

Structure Smooth

Oxidation Stability

100 hrs. @ 210 ˚ F, psi loss 2.5

Rust Prevention Rating 1,1,1

Water Washout,

 @ 175˚ F, % 2.2