**Signal Tech Air 555**

|  |
| --- |
| Product Application: |

Signal Tech Air 555 is a premium industrial grade diester synthetic compressor/vacuum pump lubricant suitable for high output precision equipment. Signal Tech Air 555 is manufactured from the highest quality pure diester basestocks and is characterized by outstanding rust protection, low deposit formation, excellent demulsibility, low air entrainment, excellent oxidation resistance, pour point and anti-foam properties.

|  |
| --- |
| Features and Advantages: |

\*Low temp fluidity

\*High temp thermal stability

\*Excellent resistance to mechanical shear

\*Compatible with Buna, Viton, Teflon

|  |
| --- |
| Package Size: |

1.0 gallon, 2.5 gallon, 5 gallon pail, 55 gallon drum

|  |
| --- |
| Typical Characteristics: |

ISO Viscosity Grade 100

Viscosity ASTM D 445

cSt @ 40°C 97.0

cSt @ 100°C 10.8

Viscosity Index 94

Copper Corrosion 1A

Specific Gravity 0.961

Flash Point, °C ASTM D93 495 (257)

Pour Point, °C ASTM D97 -30 (-34)

Autoignition Point, °F(°C) 780 (416)

Visit us at: www.beaconlubricants.com