**Beacon Signal Tech Air Tool Lubricant**

|  |
| --- |
| Product Application: |

Beacon Signal Tech Air Tool Lubricant is specially formulated for use in all types of air tool equipment such as rock drills, jackhammers, stoppers, drifters, wagon drills, chippers, tampers, riveters, pavement and breakers.

Signal Tech Air Tool Lubricant incorporates technology that allows for emulsification as well as an inherent “tackiness” that prevents water from “wetting” metal surfaces and or displacing the lubricant.

This property enables the air tools to remain “frost free” under normal operating conditions.

|  |
| --- |
| Meets or Exceeds the following Specifications: |

Gardner Denver Company

Chicago Pneumatic Tool Company

Joy Manufacturing Company

Ingersoll-Rand

|  |
| --- |
| Package Size: |

Bulk, Drums, Pails

|  |
| --- |
| Performance Features: |

\*Extreme pressure properties

\*Excellent rust protection

\*Maintains proper viscosity over a wide range of temperatures

\*Excellent wash off resistance

|  |
| --- |
| Typical Characteristics: |

**100 150 200 300**

ISO GRADE 22 32 46 68

SAE ViscosityGrade 5w 10w 10w 30w

Gravity, Degrees API 32.5 30.7 30.0 29.5

Flash Point, °F 400 400 410 420

Pour Point, °F -30 -25 -20 -20

Viscosity Index (Min.) 110 110 110 110

Viscosity

SUS @ 100 °F 115 150 240 350

SUS @ 210 °F 42 45 50 55

Color, ASTM 1.0 1.0 1.5 2.0