**Beacon Signal Kote 1105**

|  |
| --- |
| Product Application: |

Beacon Signal Kote 1105 is transparent, lightly colored oil formulated for tumbling, radiusing and deburring operations. Signal Kote 1105 utilizes food grade technical white oils for outstanding clean operation eliminating the gumming of stones, while fortified with the highest-grade rust corrosion inhibitors allowing to be used as preservative oil in indoor storage applications.

Signal Kote 1105 contains no sulfur, zinc, chlorine or phosphorus allowing it to be a truly environmentally conscious for the millennium.

|  |
| --- |
| Performance Features: |

Pleasant low odor, light viscosity, easily washable. Easily washable in alkali automated systems. Excellent preservative oil in indoor storage applications.

|  |
| --- |
| Typical Characteristics: |

Specific Gravity @ 60 °F .87

Flash Point, COC, °F 280

Pour Point, °F -20

Appearance Light

Color 2.5