**Beacon Anti-Rust 159**

|  |
| --- |
| Product Application: |

Beacon Anti-Rust 159 is premium quality transparent lightly colored water displacing non-staining rust and corrosion preventative. It is formulated using the latest approved technology in medium-bodied oils and hydro treated solvents blended with polar corrosion inhibitors, water displacing and fingerprint neutralizing agents.

Anti-Rust 159 is well suited for the thin film protection of parts between machining where water-based coolants have been used. It has a medium viscosity which assures robust coverage of metal surfaces while allowing excess fluid to drain rapidly thus allowing for a smooth efficient application with a light oil film protective layer.

Beacon Anti-Rust 159 is an excellent medium bodied rust and corrosion preventative for finished parts in dry storage or for adequately covered or bagged transport.

|  |
| --- |
| Meets or Exceeds that following Specifications: |

Military Specifications PRF16173E - Grades 2, 3

Military Specifications MIL-C-15074E

Military Specifications MIL-PFR-3150

|  |
| --- |
| Theoretical Coverage: |

3,000 sq. ft. /gallon

|  |
| --- |
| Typical Characteristics: |

Specific Gravity @ 60 °F .80

Flash Point, COC, °F 210

Pour Point, °F -20

Appearance Light Amber

Film Thickness .15

Cure Time- Approximately 2 hours

|  |
| --- |
| Corrosion Test Results: |

ASTM B-117 5 % salt spray (hours) 134

ASTM D-1748 100 % relative humidity (hours) 2300

Visit us at – www.beaconlubricants.com