**Anti-Rust 165**

|  |
| --- |
| Product Application: |

Anti-Rust 165 is an outstanding water displacing, non-staining, finger printable rust and corrosion preventative it is formulated with environmentally conscious, oxygenated, hydro carbons and calcium technology. Anti- Rust 165 provides for a highly resistant tenacious film protection with an easy to apply ether, dip or spray.

Anti-Rust 165 is very well suited for the thin film protection of parts between machining where water based coolants has been used. It has a light viscosity which assures adequate coverage of metal surfaces while allowing excess fluid to drain rapidly thus allowing for a smooth efficient application.

The thixotropic technology used in this coating allows for film building if necessary, allowing for a more useful dynamic industrial product.

|  |
| --- |
| Meets or Exceeds that following Specifications: |

MIL-C-16173E

MIL-C-22235

|  |
| --- |
| Theoretical Coverage: |

2500 square feet per gallon

|  |
| --- |
| Typical Characteristics: |

Specific Gravity @ 60 °F .83

Flash Point, COC, °F 180

Pour Point, °F -10

Appearance Light Amber

Film Thickness .06

Cure Time- Approximately 2 Hours

|  |
| --- |
| Corrosion Test Results: |

|  |  |  |  |
| --- | --- | --- | --- |
| **Humidity Cabinet –  ASTM D-1748** | **Days/Fail** | **MIL-C-16173E** | **MIL-C-22235** |
| **Film Thickness (mils)** |  | **Water Displacement** | **Sandwich Stain Test** |
| 0.03 | 40+ | Pass | Pass |
| 0.05 | 50+ | Pass | Pass |
| 0.06 | 60+ | Pass | Pass |

Visit us at – www.beaconlubricants.com