**High Pressure Pump Lubricant 10W-30**

|  |
| --- |
| Product Application: |

High Pressure Pump Lubricant 10W-30 is specially formulated API 10W-30, ISO VG 68 grade anti-wear hydraulic fluid. Designed for use in most high pressure pump crankcases such as: CAT pump, General pump, AR, Comet, Giant, Udor, and Hypro.

|  |
| --- |
| Features And Advantages: |

\*Anti-scuff, wear, foaming, oxidation and emulsification

\*High viscosity index (VI) for high and low temperature

\*Low pour point (-20 deg. Fahrenheit)

\*Exceeds wear requirements of major pump mfgs. (HFO)

\*Compatible with typically used seals

|  |
| --- |
| Typical Characteristics:  |

Viscosity, ASTM D445

 cSt @40°C 68.0

 cSt @100°C 11.3

Viscosity Index, ASTM D 2270 160

Brookfield Viscosity ASTM D 2983,

cP @ -20°C 3390

Brookefield Viscosity ASTM D2983,

cP @ -30° 16380

Brookefield Viscosity ASTM D 2983,

cP @ -40°

Tapered Roller Bearing (CEC L-45-A-00),

% Viscosity Loss 9

Density 15°C, ASTM 4052, kg/l 0.8626

Copper Strip Corrosion, ASTM D

103, 3 hours @ 100°C 1B

FZG Gear Test, DIN 51354, Fail Stage 12

Pour Point, °C ASTM D 97 -35

Flash Point, °C, ASTM D 92 240

Foam Sequence I, II, III, ASTM D 892, ml 20/0

Dielectric Strength, kV, ASTM D877

|  |
| --- |
| Package Size:  |

Bulk, Drums, Pails

Visit us at – www.beaconlubricants.com