**Signal Cut 222**

|  |
| --- |
| Product Application: |

Signal Cut 222 is an excellent heavy-duty, fully fortified full synthetic coolant that contains no chlorine, sulfur, or phosphorous compounds. Signal Cut 222 is designed for the machining of both ferrous and non-ferrous materials.

Signal Cut 222 provides excellent wetting and chip/swarf setting capabilities. This allows for uniform coolant-to-metal surface contact, important for metal surface contact important for cutting operations as well as corrosion inhibition during in-process storage.

|  |
| --- |
| Package Size: |

Drums, Pails

|  |
| --- |
| Recommended Concentrations: |

Grinding 2-3% (50:1 to 30:1)

Milling, turning, drilling, sawing 3-4% (30:1 to 25:1)

Broaching, tapping, boring 4-5% (25:1 to 20:1)

|  |
| --- |
| Features and Advantages: |

**\*** Fungicide fortified.

\* Complete oil rejecting capabilities (tramp oils).

\* Provide excellent rust protection.

|  |
| --- |
| Typical Characteristics: |

Color Clear

Specific Gravity 1.085

pH @ 20:1 Dilution 9.4

Refractometer Reading

@ 20:1 Dilution (Brix) 3.5

Visit us at – www.beaconlubricants.com