**Beacon Signal Cut 355**

|  |
| --- |
| Product Application: |

Beacon Signal Cut 355 is an environmentally conscious state of the art low odor mineral synthetic blend cutting fluid formulated for the most demanding machining applications such as but not limited to tapping, threading, broaching, gear hobbing and other like metal forming operations.

Signal Cut 355 is formulated utilizing the latest high quality pure base stocks and select chlorine free environmentally conscious additives to effectively provide the necessary medium for excellent machining performance in any and all modern heavy duty machining applications.

Because this product utilizes active sulfur and esterized technology it may discolor copper and its alloys and normally should not be used in machining these metals if staining is objectionable.

|  |
| --- |
| Package Size: |

Totes, Drums, Pails, 2 ½ gallons

|  |
| --- |
| Features and Advantages: |

\*Carbide tooling compatible

\*Excellent machining performance

\*Mist suppressant minimizes fogging/stray mist

\*May be blended with mineral oil for high or lower viscosity

\*Prevents rapid tool wear

|  |
| --- |
| Typical Characteristics:  |

Viscosity, ASTM D 445

 cSt @ 40°C 23

Flash Point, °C, ASTM D 92 180

Active Sulfur % 2.5

Synthetic Ester % 4.0

Phosphate Ester .0002

Color Amber