**Signal Cylinder 460 Oil**

|  |
| --- |
| Product Application: |

Beacon Lubricants Signal Cylinder 460 oil is a high quality full-bodied steam cylinder and worm gear lubricant. It is formulated to be thermally and shear stable utilizing robust base stocks that are compounded with high grade friction modified esters to provide a thermally and chemically stable oil that allows for excellent film strength, excellent lubricity, extended life and foam resistant.

Signal Cylinder 460 Oil is recommended for use in all types of steam cylinder applications as

well as splash lubrication worm gear sets either open or closed.

|  |
| --- |
| Package Size: |

Pails, Drums

|  |
| --- |
| Features and Advantages: |

\*Excellent metal wettability

\*Formulated to provide immediate demulsibility

\*Extended oxidation stability

\*Foam inhibited

|  |
| --- |
| Typical Characteristics:  |

Viscosity, ASTM D 445

cSt @ 40°C 460

cSt @ 100°C 30.5

Viscosity Index, ASTM D 2270 105

Pour Point, °C ASTM D 97 -6

Flash Point, °C ASTM D 92 282

Density, ASTM D4052 @ 15.6°C kg/l 0.907

Copper Strip Corrosion 1B

Visit us at – www.beaconlubricants.com