**Beacon Signal Film 015**

|  |
| --- |
| Product Application: |

Beacon Signal Film 015 is a heavy duty commercial grade after-market rust preventative formulated for use on all on and off road vehicles where extra rust and corrosion protection is required. Once applied Signal Film 015 leaves an amber encapsulated “waxy” coating that is highly resistant to high humidity and salt environments.

|  |
| --- |
| Features and Advantages: |

\*Easy to apply

\*Excellent corrosion protection

\*Non sagging thixotropic technology

\*Thins easily with mineral spirits for ease of clean up

|  |
| --- |
| Theoretical Coverage:  |

\*Average use is 1.0 – 1.5 gallons per average size vehicle.

|  |
| --- |
| Package Size: |

2.5 gallon containers, 5 gallon pails, 55 gallon drums

|  |
| --- |
| Surface Preparation & Application |

**Surface Preparation:**

\*Wash area to be coated removing salt, dirt and loose rust and oils

**Application:**

\*Signal Film 015 is formulated to be used as supplied, however if thinning is required to suit application you may thin product up to 5 % with mineral spirits. Older rustier vehicles tend to “soak” material therefore multiple successive thin coats are recommended.

|  |
| --- |
| Clean up recommendations:  |

\*Easily cleaned up with warm soapy water or mineral spirits

|  |
| --- |
| Typical Characteristics:  |

Color Dark Amber

Weight 7.4 lbs. /gallon

Film thickness 2.5 mil

Coverage 380 ft 2 p/gallon

Specific Gravity .87

Flash Point 41 °C