**Signalplex EP 0 Grease**

|  |
| --- |
| Product Application: |

Beacon Signalplex EP 0 is a high quality, industrial grade, multi-purpose lithium complex grease. This grease meets the lubrication requirements of plain and anti-friction bearings, gears, and couplings in general industrial applications. It is tough, versatile and long lasting. Beacon Signalplex EP 0 features multi-purpose use, good water resistance, high temperature performance, excellent oxidation resistance, good rust protection and fortified extreme pressure properties.

|  |
| --- |
| Package Size:  |

Drums, Kegs, Pails, Cases

|  |
| --- |
| Performance Features: |

\*Multi-purpose use

\*Good water resistance

\*High temperature oxidation resistance

|  |
| --- |
| Typical Characterisitcs: |

Color Red

NLGI Grade 0

Soap Type Lithium Complex

Structure Smooth

Penetration @ 77°C D-217

 Unworked 400

 Worked 60 Strokes 380

Dropping Point, °C D-2265 160

Timken OK Load 40

Viscosity SUS @ 100°F 800

 210°F 75

Flash Point °F 435