**Signalplex EP2 Red Grease**

|  |
| --- |
| Product Application:  |

Signalplex EP2 Red is an extended life lithium complex grease intended for use in any automotive, commercial, and industrial settings where an extended life, heavy duty, water resistant grease is required.

It is formulated with the most up to date base stocks coupled with cutting edge technology to provide for excellent high temperature performance while maintaining cold temperature pump ability.

It is formulated with water resistant tackifiers that provide excellent adhesion and structural stability coupled with a high degree of chemical and sheer stability to offer excellent corrosion protection.

|  |
| --- |
| Package Size:  |

Drums, Kegs, Pails, Tubes, 16oz. containers

|  |
| --- |
| Performance Features: |

Exceeds NLGI GC/LB.

Excellent water resistant

Superb high temperature resistance

Excellent extreme pressure properties

|  |
| --- |
| Typical Characteristics:  |

Soap Type Lithium Complex

Color Red

Structure Smooth / Tacky

Penetration at 77 °F

 60 strokes 278

 10,000 strokes 290

 100,000 strokes 298

Dropping Point, °F 506

Timken OK Load, lbs, min 60

Four Ball EP

 Weld Point Kg 250

Oxidation Stability

 100 hrs. @ 210 °F, psi loss 8.0

Rust Prevention Rating 1,1,1

Water Washout,

 @ 175 °F, % 2.1